Keystone Kool Deck ASTM Sheet

ASTM C109-77

Compressive Strength: (Using 2 inch cube specimens)


7 Days – 1300 psi (2 standard deviations)


14 Days – 1800 psi (2 standard deviations)


28 Days – 2500 psi (2 standard deviations)

ASTM C666-84

Resistance of Concrete to Rapid Freezing and Thawing:

Keystone Kool Deck: 70 cycles the flats start to fail.

ASTM C944-85

Abrasion Resistance of concrete or mortar surfaces by the Rotating - Cutter Method:

Keystone Kool Deck textured surface:


2 kg. Load – Less than 1 gm. (texture 50% flat)


6 kg. Load – Less than 3 gm. (texture 50% flat)

Mortex Manufacturing Co., Inc.

1818 W. Price Street

Tucson, AZ 85705 USA

520-887-2631     www.mortex.com

